| METAL CABLE CO. DATA SHEET |
| --- |
| No.: MC – 18042 | Date : 95.10.19 |
| Low voltage power cable Acc. IEC 60502-1( ISIRI 3569-1) , (0.6/1)1.2 kv , frequency : 50 Hz |
| Copper conductor/ XLPE insulated/ pvc bedding/ galvanized steel wire armour/ pvc outer sheath Cable code : N2XRY-O |
| R | SPECIFICATION |
| 1 | Cable size | 7x1.5mm2 |
| 2 | Conductor | material | Plain annealed copper |
|  |  | Class | 2 , round |
|  |  | construction | 7x0.53 mm |
| 3 | Insulation | material | XLPE |
|  |  | operation temp. | 90°C |
|  |  | thickness | 0.7 mm |
|  |  | colour | Red , yellow , black N: white |
| 4 | Bedding | material | PVC |
|  |  | operation temp. | 90°C |
|  |  | thickness | 1.0 mm |
|  |  | colour | Black |
| 5 | Armour | material | Galvanized steel |
|  |  | type | Wire armour (GSWA ) |
|  |  | diameter | 1.2 mm |
| 6 | Outer jacket | material | PVC |
|  |  | operation temp. | 90°C |
|  |  | thickness | 1.8 mm |
|  |  | colour | Black |
| 7 | Overall diameter approx. | 17.0 mm |
| 8 | Max. dc conductor resistance at 20°C | 7.41 Ω/km acc. IEC 60228 |
| 9 | Max. ac conductor resistance at 90°C | 9.49 Ω/km |
| 10 | Min. Insulation resistance at 90 °C | 0.841 MΩ . km |
| 11 | Short circuit current | 0.357 kA at 1 second |
| 12 | High voltage test | 3.5 kvac or 8.4 kvdc for 5 min |
| 13 | Working temperature | -25 ____ +90 °C |
| 14 | Min. bending radius | 6 x D (Overall diameter) |
| 15 | Flame retardant test | As per IEC 60332-1 |
| 16 | Cable length (per drum) | 2000 M |
| 17 | Cable weight approx. | 620 kg/km |
| Marking : METAL CABLE CO. IEC 60502 N2XRY 7x1.5 SQMM 0.6/1 KV MADE IN IRAN 1395 |

Technical approval